## Slide 3
There are no physicists in America.
----Paul Dirac

## Slide 5
It doesn't matter how beautiful your theory is, it doesn't matter how smart you are.
If it doesn't agree with experiment, it's wrong.
----Richard Feynman

## Slide 6
It doesn't matter how beautiful your theory is, it doesn't matter how smart you are.
If it doesn't agree with experiment, it's wrong.
----Richard Feynman

## Slide 8
Near-field Nano-imaging and Nano-spectroscopy of Percolating Thin Gold Films
Xinzhong Chen
Department of Physics and Astronomy Stony Brook University
March, 16 2017

## Slide 9
The optical properties of metal nanoparticles have long been of interest, which dates back to Faraday’s investigations of colloidal gold in the mid 1800s.
Background

## Slide 10
Mie presented a solution to Maxwell’s equations that describes the extinction spectra of spherical particles of arbitrary size.

## Slide 11
Can we understand the optical behaviors if the geometry of particles are disordered and semi-random?
Question
AFM image of dimension 10 µm taken from one of the samples.

## Slide 12
Sample Introduction
A set of nine sputtered gold thin films (thickness~30 nm) on sapphire substrate.
Each film has slightly different surface filling fraction.
Four films are slight below percolation threshold and five are slightly above percolation threshold. Films DC conductivity from 22 Ω to kΩ range to MΩ range to infinite.
Scanning electron micrographs of 4mm by 4mm areas of three granular gold films spanning percolation.

## Slide 13
Mid-IR Broad-Band Reflectance Spectroscopy
Mid-IR Broad-Band Near-Field Spectroscopy
Mid-IR Single-Wavelength Near-Field Imaging
Experiments and Data

## Slide 14
Reflectance Spectroscopy
Experimental reflectance spectrum measured at ALS, Berkeley, CA.

## Slide 15
Reflectance Spectroscopy
Experimental reflectance spectrum measured at ALS, Berkeley, CA.
Effective Medium Approximation
where

## Slide 16
Reflectance Spectroscopy
Experimental reflectance spectrum measured at ALS, Berkeley, CA.
Simulation of reflectance spectrum by effective medium theory.

## Slide 17
Broad-Band Near-Field Spectroscopy
AFM
IR Near-field Probe
2-25 um
Schematics of near-field
spectroscopy
Near-field spectrum of film #6
Near-field spectrum of film #7
Near-field spectrum of film #10

## Slide 18
High q Effect
Selected near-field spectrum
Selected near-field spectrum

## Slide 19
High q Effect
Selected near-field spectrum
Selected near-field spectrum

## Slide 20
High q Effect
Selected near-field spectrum
Simulation by mixing spectra of non-zero in-plane momenta
Simulation by mixing spectra of non-zero in-plane momenta
Selected near-field spectrum

## Slide 21
Mid-IR Single-Wavelength Near-Field Imaging
AFM
IR Near-field Probe
~10 um
Schematics of near-field
imaging.
AFM topography image
Real part of near-field signal
Imaginary part of near-field signal

## Slide 22
Mid-IR Single-Wavelength Near-Field Imaging
AFM
IR Near-field Probe
~10 um
Schematics of near-field
imaging.
AFM topography image
Real part of near-field signal
Imaginary part of near-field signal

## Slide 23
Mid-IR Single-Wavelength Near-Field Imaging
AFM
IR Near-field Probe
~10 um
Schematics of near-field
imaging.
AFM topography image
Real part of near-field signal
Imaginary part of near-field signal

## Slide 24
Mid-IR Single-Wavelength Near-Field Imaging
AFM
IR Near-field Probe
~10 um
Schematics of near-field
imaging.
AFM topography image
Real part of near-field signal
Imaginary part of near-field signal

## Slide 25
Extract of Local Dielectric Constant
Real part of near-field signal
Real part of near-field signal
Imaginary part of near-field signal
Imaginary part of near-field signal
Real part of local dielectric constant
Real part of local dielectric constant
Imaginary part of local dielectric constant
Imaginary part of local dielectric constant

## Slide 26
Software Simulation
CST model of gold sphere on SiO2 substrate
Simulated surface electric field distribution
Simulated surface photo-current distribution

## Slide 27
Summary
  Near percolation threshold, slight filling fraction difference can cause large optical property difference both locally and globally.
  Far-field spectra can be understood by effective medium approximation.
  Near-field spectra can be qualitatively explained by high q effect.
  Local near-field signal variation is observed. Local dielectric constant can be semi-quantitatively extracted.
  Relationship between local topography and optical properties reminds to be studied.

## Slide 28
References

## Slide 30
CST: Leo, William, Matthew, Jack
Matlab: Alex Stephanie
SNOM: Jiawei
Samples and ALS data: Larry
Overall guidance: Mengkun
Acknowledgement